## Slide 1: Tensile testing of Ti-6Al-4V alloy superplasticity
Sergey Aksenov, Ph.D.

## Slide 2: Introduction
As a titanium alloys have remarkable properties in terms of mechanical characteristics, low density and elevated corrosion resistance, it is widely used in many fields including aerospace, automotive, electronics and even bio-medical industry. At the same time the semi-finished parts of titanium alloys are rather expensive in particular because of the number and complexity of technological operations. The superplastic forming (SPF) is an effective way to manufacture very complex thin-shape components, which allows at the same time to decrease its cost.
The major advantages of SPF:
The possibility of form a large and complex workpieces in one operation
Excellent precision of a finished products
Fine surface finish of a products

## Slide 3: Typical titanium alloys SPF applications

## Slide 4: Material
Ti-6Al-4V is the most popular titanium alloy which covered more than 50% of titanium alloy production
Physical properties:
Density 4.42 g/cm3
Melting Range 1649±15 °C
Specific Heat 560 J/(kg °C)
Mechanical properties:
Tensile Strength 1000 Mpa
Elastic Modulus 114 Gpa
Chemical composition
C
Fe
N2
O2
Al
V
H2
Ti
< 0.08%
< 0.25%
< 0.05%
< 0.2%
5.5-6.76%
3.5-4.5%
< 0.015%
Balance

## Slide 5: Constitutive model
The main goal of the mechanical properties investigation for an alloy in the hot forming state is the establishment of the relationship:
,
where is the flow stress, – effective strain rate, ε – effective strain and
– temperature.
Backofen equation:
where
K – material constant,
m – strain-rate sensitivity exponent

## Slide 6: Constitutive model
O. M. Smirnov proposed the rheological model of elasto-visco-plastic (EVP) medium which describes the behavior of superplastic materials in a wide range of strain rates.

## Slide 7: Constitutive model
The strain rate sensitivity exponent

## Slide 8: Dynamic materials model
Y.V.R.K. Prasad et al. suggested the dynamic materials modeling (DMM) approach for describing the material behavior under processing conditions by means of processing maps.
Efficiency of power dissipation:
Instability criterion (Zingler):

## Slide 9: Dynamic materials model
Y.V.R.K. Prasad et al.
()
Narayana Murty
()
Efficiency of power dissipation
Instability criterion

## Slide 10: Experiment
As received Ti-6Al-4V alloy was used in the investigation. Each specimen was set in clamps of the test machine, placed in the furnace and heated up to the preset temperature. Then isothermal tensile-tests were carried out in the temperature range of 700 – 925 °С.

## Slide 11: Stress-strain rate curves
The experimental (markers) and predicted (solid lines) stress-strain curves obtained by stepped tensile-tests

## Slide 12: Stress-strain rate curves
Chart: T, 0C
| 700 | 725 | 750 | 775 | 800 | 825 | 850 | 875 | 900 | 925 | 950
Ss | 128.4216 | 118.9781 | 153.9539 | 132.7353 | 142.8025 | 95.4395 | 119.0735 | 92.0972 | 78.48 | 77.004 | 60.1362
S0 | 22.0644 | 19.6661 | 12.6082 | 11.108 | 8.6069 | 9.5723 | 10.4266 | 10.3803 | 7.4967 | 3.7607 | 10.921
Chart: T, 0C
| 700 | 725 | 750 | 775 | 800 | 825 | 850 | 875 | 900 | 925 | 950
Ss | 128.4216 | 118.9781 | 153.9539 | 132.7353 | 142.8025 | 95.4395 | 119.0735 | 92.0972 | 78.48 | 77.004 | 60.1362
S0 | 22.0644 | 19.6661 | 12.6082 | 11.108 | 8.6069 | 9.5723 | 10.4266 | 10.3803 | 7.4967 | 3.7607 | 10.921

## Slide 13: Stress-strain rate curves
Chart: T, 0C
| 700 | 725 | 750 | 775 | 800 | 825 | 850 | 875 | 900 | 925 | 950
K | 203244.3672 | 140433.2846 | 163942.2162 | 140207.7305 | 105390.0782 | 40965.4787 | 23362.908 | 12021.7806 | 10464.4592 | 7334.8283 | 3462.511
Chart: T, 0C
| 700 | 725 | 750 | 775 | 800 | 825 | 850 | 875 | 900 | 925 | 950
K | 203244.3672 | 140433.2846 | 163942.2162 | 140207.7305 | 105390.0782 | 40965.4787 | 23362.908 | 12021.7806 | 10464.4592 | 7334.8283 | 3462.511

## Slide 14: Stress-strain rate curves
Chart: T, 0C
| 700 | 725 | 750 | 775 | 800 | 825 | 850 | 875 | 900 | 925 | 950
mv | 2.0718 | 1.8657 | 1.2624 | 1.1987 | 1.0814 | 1.3603 | 1.3038 | 1.3303 | 1.3215 | 1.3123 | 1.6131

## Slide 15: Strain rate sensitivity exponent

## Slide 16: Optimum strain rate

## Slide 17: Efficiency of power dissipation

## Slide 18: Processing maps
Prasad
Narayana Murty

## Slide 19: Maximum of

## Slide 20: Tension at 825 °C
Chart: Strain
rate 5.7e-4 | 20.5673 | 24.5672 | 27.7219 | 30.0247 | 31.7081 | 33.0246 | 34.086 | 34.954 | 35.7193 | 36.3808 | 37.0084 | 37.5823 | 38.1416 | 38.6692 | 39.1763 | 39.6624 | 40.1337 | 40.5825 | 41.0112 | 41.4064 | 41.771 | 42.1049 | 42.4126 | 42.6917 | 42.9574 | 43.2019 | 43.4337 | 43.6474 | 43.8605 | 44.0673 | 44.2784 | 44.491 | 44.7127 | 44.9493 | 45.1816 | 45.4237 | 45.6645 | 45.9193 | 46.1617 | 46.3864 | 46.5805 | 46.7419 | 46.8721 | 46.9779 | 47.0366 | 47.0316
rate 3.8e-4 | 21.2331 | 25.0817 | 27.648 | 29.2784 | 30.4916 | 31.524 | 32.466 | 33.3616 | 34.2373 | 35.1093 | 35.9637 | 36.7846 | 37.5713 | 38.3342 | 39.0645 | 39.7588 | 40.3898 | 40.9839 | 41.5162 | 42.0077 | 42.4584 | 42.8788 | 43.269 | 43.6341 | 43.9686 | 44.2783 | 44.5636 | 44.8295 | 45.0759 | 45.3027 | 45.5065 | 45.6857 | 45.8355 | 45.9558 | 46.0435 | 46.0922 | 46.0949 | 46.044
rate 2e-4 | 21.3198 | 24.5001 | 27.1033 | 29.2516 | 31.0682 | 32.6807 | 34.143 | 35.4404 | 36.6138 | 37.6473 | 38.584 | 39.3974 | 40.1158 | 40.7489 | 41.2943 | 41.7578 | 42.1643 | 42.5627 | 42.9804 | 43.443 | 43.9794 | 44.6081 | 45.3482
rate 1e-4 | 16.7235 | 22.6963 | 27.5967 | 31.0407 | 34.0235 | 36.1951 | 37.7191 | 38.784 | 39.6617 | 40.1328 | 37.52
Optimum = 3.8e-4

## Slide 21: Tension at 875 °C
Chart: Strain
| 7.3810000000000001E-2 | 0.14618999999999999 | 0.21612999999999999 | 0.28251999999999999 | 0.34511999999999998 | 0.40332000000000001 | 0.45800000000000002 | 0.50905999999999996 | 0.55720000000000003 | 0.60270000000000001 | 0.64642999999999995 | 0.68855999999999995 | 0.72885 | 0.76715 | 0.80357000000000001 | 0.83848999999999996 | 0.87219999999999998 | 0.90495999999999999 | 0.93735000000000002 | 0.96902999999999995 | 1 | 1.0293699999999999 | 1.0576700000000001 | 1.08473 | 1.1110500000000001 | 1.13653 | 1.1615599999999999 | 1.18614 | 1.21041 | 1.23407 | 1.2571600000000001 | 1.2796000000000001 | 1.30165 | 1.3232699999999999 | 1.3446800000000001 | 1.3656999999999999 | 1.38635 | 1.4061999999999999 | 1.4255 | 1.4441299999999999 | 1.4624999999999999 | 1.4803900000000001 | 1.4980899999999999
rate 2.88e-3 | 30.9205 | 40.0543 | 44.3683 | 46.6093 | 47.7302 | 48.3409 | 48.8139 | 49.1748 | 49.5031 | 49.7083 | 49.8021 | 49.7915 | 49.6749 | 49.5948 | 49.6778 | 49.6625 | 49.607 | 49.5037 | 49.3514 | 49.1562 | 48.9322 | 48.6921 | 48.4422 | 48.1873 | 47.9195 | 47.6323 | 47.3174 | 46.9698 | 46.583 | 46.1558 | 45.6839 | 45.1682 | 44.5981 | 43.9596 | 43.2506 | 42.4746 | 41.5528 | 40.3696 | 38.7916 | 36.7199 | 34.2819 | 31.3663 | 28.0259
rate 1.9e-3 | 27.1419 | 35.5095 | 37.6755 | 39.3899 | 40.4655 | 41.3616 | 42.093 | 42.6817 | 43.1466 | 43.5126 | 43.787 | 43.9834 | 44.1005 | 44.1384 | 44.0869 | 43.9328 | 43.6599 | 43.2501 | 42.6875 | 42.0004 | 41.1885 | 40.1467 | 39.2342 | 38.0328 | 36.9437 | 36.1305 | 34.2049 | 32.4418 | 28.0751 | 23.5057
rate 5e-4 | 15.1593 | 16.4944 | 17.5985 | 18.5551 | 19.398 | 20.2314 | 21.0198 | 21.7668 | 22.4745 | 23.137 | 23.7632 | 24.3533 | 24.9146 | 25.4465 | 25.9485 | 26.4247 | 26.8816 | 27.3123 | 27.7218 | 28.1122 | 28.4859 | 28.8458 | 29.1938 | 29.5501 | 29.9078 | 30.263 | 30.5764 | 30.8551 | 31.107 | 31.3546 | 31.6 | 31.8463 | 32.0884 | 32.3309 | 32.5701 | 32.8072 | 33.0388 | 33.2628 | 33.4775 | 33.6832 | 33.8782 | 34.0609 | 34.2294 | 34.3827 | 34.521 | 34.6497 | 34.7526 | 34.8362 | 34.9002 | 34.9438 | 35.1114 | 35.1652 | 35.1679 | 35.0355 | 34.9708
rate 3e-4 | 10.4388 | 12.5473 | 14.4444 | 16.2089 | 17.7166 | 18.9907 | 20.215 | 21.2257 | 22.2364 | 23.1668 | 24.0105 | 24.8163 | 25.5787 | 26.3012 | 26.9882 | 27.6423 | 28.2677 | 28.8664 | 29.4396 | 29.9855 | 30.5033 | 30.9893 | 31.4451 | 31.8693 | 32.2602 | 32.694 | 33.1343 | 33.5571 | 33.9767 | 34.3691 | 34.7304 | 35.0557 | 35.3494 | 35.6101 | 35.8344 | 36.0144 | 36.1607 | 36.2712 | 36.3487 | 36.3945 | 36.4092 | 36.392 | 36.3297 | 36.1676 | 35.8489 | 35.3186 | 34.4752 | 32.858
Optimum = 8.54e-4

## Slide 22: Tension at 925 °C
Optimum = 1.4e-3
Chart: Strain
| 5.4420000000000003E-2 | 0.10602 | 0.15365000000000001 | 0.19888 | 0.24252000000000001 | 0.28483999999999998 | 0.32525999999999999 | 0.36338999999999999 | 0.39973999999999998 | 0.43453999999999998 | 0.46814 | 0.50087999999999999 | 0.53281999999999996 | 0.56530999999999998 | 0.59589999999999999 | 0.62573999999999996 | 0.65342999999999996 | 0.68079000000000001 | 0.70689999999999997 | 0.73241999999999996 | 0.75722 | 0.78198999999999996 | 0.80615999999999999 | 0.83003000000000005 | 0.85296000000000005 | 0.87543000000000004 | 0.89736000000000005 | 0.91912000000000005 | 0.96157999999999999 | 0.98216999999999999 | 1.0022599999999999 | 1.0210999999999999 | 1.0400700000000001 | 1.0581700000000001 | 1.1116600000000001
rate 4.4e-3 | 24.8597 | 31.2229 | 34.1831 | 35.8882 | 36.9592 | 37.7832 | 38.4547 | 39.0033 | 39.4617 | 39.8412 | 40.1517 | 40.3983 | 40.5849 | 40.7132 | 40.7828 | 40.8065 | 40.7931 | 40.7537 | 40.6936 | 40.614 | 40.4971 | 40.3257 | 40.0976 | 39.8152 | 39.4817 | 39.0929 | 38.6331 | 38.0527 | 37.3748 | 36.7696 | 36.0775 | 35.3072 | 34.4723 | 33.3131 | 29.6315
rate 2.9e-3 | 21.9453 | 27.2181 | 29.9335 | 31.8728 | 33.2017 | 34.2003 | 35.0727 | 35.8147 | 36.4478 | 36.984 | 37.4412 | 37.811 | 38.0925 | 38.2872 | 38.3976 | 38.4243 | 38.3681 | 38.326 | 38.271 | 38.2153 | 38.1596 | 38.0632 | 37.9411 | 37.8368 | 37.725 | 37.5891 | 37.4315 | 37.1537 | 36.8024 | 36.3401 | 35.6723 | 34.6384 | 32.9935 | 30.5686 | 27.4646
rate 1.4e-3 | 14.9136 | 19.7858 | 23.215 | 26.0917 | 28.4503 | 30.2536 | 31.545 | 32.6224 | 33.6074 | 34.5364 | 35.4091 | 35.7238 | 35.8061 | 35.6817 | 35.3108 | 34.7242 | 33.8587 | 32.6826
rate 1e-3 | 14.3503 | 20.8884 | 24.5254 | 27.4339 | 29.5012 | 31.0049 | 31.9273 | 32.7954 | 33.0248 | 33.0906 | 32.8655 | 32.1854 | 30.5764 | 26.672 | 18.5219 | 7.4497
rate 3e-4 | 6.1652 | 9.5736 | 11.2658 | 13.5829 | 14.8871 | 16.4187 | 17.9321 | 19.2558 | 20.5014 | 21.5608 | 22.6259 | 23.6109 | 24.5186 | 25.2946 | 25.9803 | 26.628 | 27.1989 | 27.7036 | 28.1461 | 28.5223 | 28.8026 | 28.9322 | 28.8037 | 28.2765

## Slide 23: Stress-strain curves
Chart: Effective strain [-]
800 | 26.3403 | 30.3868 | 34.0166 | 37.096 | 39.5789 | 41.5419 | 43.0775 | 44.3089 | 45.3125 | 46.1708 | 46.9323 | 47.6324 | 48.2777 | 48.8733 | 49.4143 | 49.8918 | 50.3044 | 50.6623 | 50.9752 | 51.2468 | 51.4766 | 51.6643 | 51.7932 | 51.862 | 51.8764 | 51.837 | 51.748 | 51.6168 | 51.443 | 51.2336 | 50.9975 | 50.7415
825 | 21.2331 | 25.0817 | 27.648 | 29.2784 | 30.4916 | 31.524 | 32.466 | 33.3616 | 34.2373 | 35.1093 | 35.9637 | 36.7846 | 37.5713 | 38.3342 | 39.0645 | 39.7588 | 40.3898 | 40.9839 | 41.5162 | 42.0077 | 42.4584 | 42.8788 | 43.269 | 43.6341 | 43.9686 | 44.2783 | 44.5636 | 44.8295 | 45.0759 | 45.3027 | 45.5065 | 45.6857 | 45.8355 | 45.9558 | 46.0435 | 46.0922 | 46.0949 | 46.044
850 | 19.9282 | 21.1903 | 22.9872 | 23.9536 | 24.8659 | 25.8878 | 26.7305 | 27.5339 | 28.3054 | 29.453 | 30.1792 | 30.8937 | 31.5985 | 32.296 | 33.0007 | 33.701 | 34.3946 | 35.0788 | 35.7497 | 36.4041 | 37.0383 | 37.6505 | 38.2376 | 38.5615 | 38.7314 | 39.2328 | 39.7016 | 39.9377 | 40.3398 | 40.7089 | 41.0446 | 41.0481 | 41.321 | 41.5639 | 41.7779 | 41.7634 | 41.9241 | 42.0611
925 | 14.9136 | 19.7858 | 23.215 | 26.0917 | 28.4503 | 30.2536 | 31.545 | 32.6224 | 33.6074 | 34.5364 | 35.4091 | 35.7238 | 35.8061 | 35.6817 | 35.3108 | 34.7242 | 33.8587

## Slide 24: Stress-strain rate curves
Chart: Temperature [°C]
| 750 | 775 | 800 | 825 | 850 | 875 | 900 | 925 | 950
0.2 | 37.2909 | 37.8229 | 32.5148 | 26.4513 | 23.9677 | 22.8009 | 22.0538 | 16.7834 | 21.3557
0.6 | 53.0732 | 51.2225 | 45.4448 | 37.0979 | 33.2222 | 31.2332 | 29.4852 | 28.1016 | 31.6741
1 | 59.7285 | 58.5074 | 51.075 | 44.6318 | 41.0567 | 37.7427 | 35.8986 | 34.4581 | 38.0969
stepped | 44.3 | 43.3 | 36.4 | 34.6 | 29.5 | 28.6 | 27.1 | 22.5 | 21.7 | 19 | 23.6

## Slide 25: Summary
The strain-rate ranges which ensure the realization of superplasticity at forming of Ti-6Al-4V alloy were determined in the range of temperatures 700-925 °C.
At the relatively low temperatures 700–775 °C the Ti-6Al-4V alloy shows all signs of superplasticity if strain-rates do not exceed 10-5 s-1.
Maximization of energy dissipation efficiency, which was calculated by the simplified Prassad formula, leads automatically to maximize the strain rate sensitivity index .
The method proposed by Narayana Murty, based on the same theoretical preconditions, but differs in that it does not use a priori assumptions about the nature of the exponential curve and lays a claim to be more adequate. At the same, strain rate, which provides maximum of energy dissipation efficiency calculated according his approach does not provide the maximum of .

## Slide 26: Thank you for your attention!